The following Tile Guide Specification is an excerpt from the 2002 Specification Guide 09300 Tile Installation Manual.

Tile Guide Specification

(name)

1.	General

1.1	SECTION INCLUDES

1.1.1	Floor tile

1.1.2	Wall tile

1.1.3	Ceiling tile

1.1.4	Tile base, treads and trim.

1.2	RELATED SECTIONS

SPEC NOTE: Edit to suit.

1.2.1	Section [03300 – Cast In Place Concrete:] [03350 – Concrete Finishing:] concrete floor 					finishing.

1.2.2	Section 05510 – Metal Stairs: tred reinforcing.

1.2.3	Section 06100 - Rough Carpentry: plywood sub floor and underlayment.

1.2.4	Section 07900 – Joint Sealers.

1.2.5	Section 09250 – Gypsum Board: [gypsum board] [cementitious backer unit] [coated glass mat 				backer board]

SPEC NOTE: Edit to suit project requirements.  Delete standards that do not apply to the project.

1.3 REFERENCES

1.3.1	ASTM A82/185: Reinforcing Welder Galvanized Wire Fabric/Mesh.

1.3.2	ANSI A108-1999: American National Standard Specification for the Installation of Ceramic Tile.

1.3.3	ANSI A118.1-1999: Dry-Set Portland Cement.

1.3.4	ANSI A118.2-1999: Conductive Dry-Set Portland Cement Mortar.

1.3.5	ANSI A118.3-1999: Water Cleanable Tile Setting and Grouting Epoxy.

1.3.6	ANSI A118.4-1999: Latex-Portland Cement Mortar.

1.3.7	ANSI A118..5-1999: Furan Mortars and Grouts.

1.3.8	ANSI A118.6-1999: Ceramic Tile Grouts.

1.3.9	ANSI A118.7-1999: Polymer Modified Cement Grouts.

1.3.10	ANSI A118.8-1999: Modified Epoxy Emulsion Mortar/Grout.

1.3.11	ANSI A118.9-1999: Cementitious Backer Units (CBU).

1.3.12	ANSI A118.10-1993: Load Bearing, Bonded, Waterproof Membrane for Thin-set Ceramic Tile and

Dimensional Stone Installations.

1.3.13	ANSI A118.11-1999: Exterior Grade Plywood (EGP) Latex-Portland Cement Mortar.

1.3.14	ANSI A136.1-1999: Organic Adhesive.

1.3.15	ASTM C144-99: Standard Specification for Masonry Aggrenates.

1.3.16	ASTM C207-91 (1992): Standard Specification for Hydrated Lime.

1.3.17	ASTM C503-99: Standard Specification for Marble Dimension Stone.

1.3.18	ASTM C568-99: Standard Specification for Limestone Dimension Stone.

1.3.19	ASTM C615-99: Standard Specification for Granite Dimension Stone.

1.3.20	ASTM C627-93: Standard Method for Evaluating Ceramic Floor Tile Installation Systems.

1.3.21	ASTM C648-84: Standard Test Method for Breaking Strength of Ceramic Tile.

1.3.22	ASTM C241: Abrasion Resistance.

1.3.23	ASTM C36-97: Gypsum Board.

1.3.24	ASTM C616-99: Standard Specification for Quartz-Based Dimension Stone.

1.3.25	ASTM C629-99: Standard Specification for Slate Dimension Stone.

1.3.26	ASTM C847-95: Standard Specification for Reinforcing Metal Lath.

1.3.27	ASTM C1028-89: Standard Test Method for Evaluating the Static Coefficient of Friction of Ceramic 			Tile.

1.3.28	ASTM C1178-96: Glass Mat Water Gypsum backing Board.

1.3.30	ASTM C171 D4397 ASTM D226: Cleavage Membrane.

1.3.31	CAN/CSA-A5-93: Portland Cement.

1.3.32	CSA A123.3-98: Asphalt Saturated Organic Roofing Felt.

1.3.33	CSA O121-M1978: Exterior Grade Douglas Fir Plywood.

1.3.34	CSA 0151: Canadian Softwood Plywood.

1.3.35	CSA 0153: Poplar Plywood.

1.3.36	CAN/CSA-0325.0: Construction Sheathing.

1.3.37	CSA 0437.0: Oriente Strandboard.

1.3.38	CAN/CGSB-25.20-95: Surface Sealer for Floors.

1.3.39	CAN/CGSB-51.34-M86: Vapour Barrier, Polyethylene Film for Use in Building Construction.

1.3.40	CAN/CGSB-75.1M88: Tile, Ceramic.

1.3.41	CAN/ULC 5701 Type 4: Rigid Polystyrene Insulation.

1.3.42	Terrazzo, Tile & Marble Association of Canada (TTMAC): Tile Spceification Guide 09300-2002.

1.3.43	Terrazzo, Tile and Marble Association of Canada 2000 Maintenance Guide.

1.4	PERFORMANCE STANDARDS

1.4.1	Static Coefficient of Friction: Tile installed on walkway surfaces shall have the following values as 			determined by testing identical products per ASTM C1028.

1.4.1.1		Level Surfaces: Minimum 0.5 dry.

1.4.1.2		Step Treads: Minimum 0.6 dry.

1.4.1.3		Ramp Surfaces: Minimum 0.6 dry.

SPEC NOTE: Tile as well as total assembly must be able to meet or surpass the testing requirements under conditions similar to actual specified usage or environments.

1.4.2	Traffic Level Performance: floor tiles to moot [extra heavy] [heavy] [moderate] [light] [residential] 			traffic level performance passing ASTM C627, cycle 1 trough [14] [12] [10], as described in TTMAC 			Tile Specification Guide 09300.

1.4.2.1		Extra Heavy: Passes cycle 1 through 14.

1.4.2.2		Heavy: Passes cycle 1 through 12.

1.4.2.3		Moderate: Passes cycle 1 through 10.

1.4.2.4		Light: Passes cycle 1 through 6.

1.4.2.5		Residential: Passes cycle 1 through 3.

1.4.3	Exterior tiles provided for Work in this Section to be frost resistant in accordance with CAN/CGSB-			75.1 and shall have a moisture absorption rating of 3.0% or less.

SPEC NOTE: Specific quantity and size of samples required and whether they are to be mounted on panels, with specified grout.

1.5	SAMPLES

1.5.1	Submit samples to requirements of Section [01300] [01001].

1.5.2	Samples: [305 x 305] [__ x __] mm size panel [c/w approved grout colour]; mounted to a [19] [___] 			mm thick plywood backer.

SPEC NOTE: Shop drawing are generally only required for usual conditions such as tile for pools, special mosaics and other installations requiring details.

1.6	SHOP DRAWINGS

1.6.1	Submit shop drawings to requirements of Section [01001] [01300] [____].

1.6.2	Shop Drawings: indicate terminal, targets and special patterns. Include location and details for all 			proposed control joints.

1.7	SUBMITTALS

1.7.1	Submit four copies of TTMAC Maintenance Guide for inclusion in the operation and maintenance 			manual prepared and submitted in Section [01001] [01700]. Give specific warning of any 				maintenance practice or materials that may damage or disfigure the finish work.

1.7.2	Submit product data [and WHMIS MSDS] sheets for floor sealer products [if required by the stone or 			grout].

1.7.3	Where more than one manufacturer’s product are part of a single tile assembly, arrange for each 			manufacturer to submit a written statement of compatibility with respect to the other manufacturer’s 			materials [if required].

SPEC NOTE: Include which provide the criteria, limitations and standards to establish a minimum level of quality that manufacturers’ and application can be evaluated for compliance with requirements of the project.

1.8	QUALITY ASSURANCE [if required]

1.8.1	Installer: Employ skilled mechanics trained and experienced in tile work, company must be 				registered as members in good standing with the Terrazzo, Tile and Marble Association of Canada, 			with a minimum of two years [proven] experience. If requested by Consultant, submit a listing of at 			least three previously completed projects of similar size and scope.

1.8.2	Supplier: A member with good standing with the Terrazzo, Tile and Marble Association of Canada, 			providing materials meeting the minimum standards of TTMAC.

1.8.3	Consultant: Specification and compatibility to be submitted to the TTMAC through the Verispec 				Program. Cost to be carried by the trade contractor.

1.9	ENVIRONMENTAL CONDITIONS

1.9.1	Do not install tiles at temperatures less than [12 degrees C] [55 degrees F] or above [35 degrees C] 			[100 degrees F].

1.9.2	Maintain temperatures at or above [12 degrees C] [55 degrees F] until cementitious materials have 			fully cured.

1.9.3	Do not apply epoxy mortar and grouts at temperatures below [18 degrees C] [65 degrees F] or 				above [35 degrees C] [95 degrees F].

1.10	DEVIVERY STORAGE AND HANDLING

1.10.1	Store materials in a dry area, protected from freezing, staining and damage.

1.10.2	Store cementitious materials on a dry surface.

1.11	EXTRA MATERIALS

1.11.1	Provide extra stock to requirement of Section [01700] [01001].

1.11.2	Extra Stock: [4 m2] [40 ft2] or 2 percent, whichever is the greater, of each type and colour of tile; 			clearly marked to identify:

1.11.2.1	Manufacturer’s name

1.11.2.2	Product’s name

1.11.2.3	Product colour and pattern

1.11.2.4	Batch and Dye Lot #

1.11.3	Package tile products neatly in original containers, to prevent damage.

2.	Products

2.1	MANUFACTURERS

2.1.1	Manufacturers of [ceramic] [granite] [limestone] [marble] [slate] tile having Product considered 				acceptable for use:

2.1.1.1		[____]

2.1.1.2		[____]

2.1.2	Manufacturer of mortar and grout having Product considered acceptable for use:

2.1.2.1		[____]

2.1.2.2		[____]

2.1.2.3		[____]

2.1.3	Substitutions: refer to instruction to Bidders and Section [01600] [01001] [____].

SPEC NOTE: Preselect and name exact tile, stair treads and/or trim required wherever possible. Otherwise specify standard, type, class, size, colour and pattern. Refer to TTMAC Tile Specification Guide 09300/2002.

2.2	TILE MATERIALS

2.2.1	Ceramic [Floor] [Wall] Tile [__x__] mm size [___] mm thick; to CAN/CGSB-75.1-M Tyle Consultant.

2.2.2	Marble Tile: [__x__] mm size, [___] mm thick; to ASTM. C503; [____] by [____]. [____] colour [as 			selected by  Consultant].

2.2.3	Limestone: [__x__] mm size, [___] mm thick; to ASTM C568. Class III – High Density; [____] by 			[____]. [____] colour [as selected by  Consultant].

2.2.4	Granite Tile: [__x__] mm size, [___] mm thick; to ASTM C615. [____] by [____]. [____] colour [as 			selected by  Consultant].

2.2.5	Slate Tile: [__x__] mm size, [___] mm thick; to ASTM C615. [____] by [____]. [____] colour [as 				selected by Consultant].

2.2.6	Base: coved; type, size, colour and texture to match adjacent flooring material.

2.2.7	Stair Treads: bull nosed edge, [non-slip surface], matching floor tile, sized to suit stair tread 				configuration.

SPEC NOTE: t it recommended the following materials are supplied by a single source manufacturer.

2.3	MORTAR

2.3.1	Portland Cement: to CAN/CSA-A5, Type 10.

2.3.2	Hydrated Lime: to ASTM C207, Type [N] [NA] [S] [SA].

2.3.3	Sand: to ASTM C144, passing 16 mesh.

2.3.4	Dry-Set Portland Cement Mortar: to ANSI A188.1.

2.3.5	Latex Portland Cement Mortar: to ANSI A118.4.

2.3.6	Commercial Portland Cement Grout: to ANSI A118.6.

2.3.7	Latex Portland Cement Grout: to ANSI A118.6.

2.3.8	Polymer Modified Grout: to ANSI A118.7.

2.3.9	Epoxy Adhesive and Grout: to ANSI A118.3.

2.3.10	Modified Epoxy Emulsion Mortar: to ANSI A118.8.

2.3.11	Furan Mortars and Grout: to ANSI A118.5.

2.3.12	Exterior Grade Plywood (EGP) Latex Portland Cement Mortar: to ANSI A118.11.

2.3.13	Organic Adhesive: to ANSI A136.1.

2.4	ACCESSORIES

2.4.1	Underlayment: [as specified under Section 06100.] [16 mm] [5/8’’] thick Douglas Fir plywood, to CSA 			O121

2.4.2	Cleavage Membrane: [0.10 mm] [4 mil] thick polyethylene film, to CAN/CGSB-51.34-M] [asphalt 			saturated roofing felt, to CSA A123.3, Type 1].

2.4.3	Metal Lath: galvanized type, 1.4 kg/m3 to ASTM C847.

2.4.4	Reinforcing Mesh: [51 x 51 mm] mesh size fabricated from 1.6 mm thick galvanized steel wire; 				welded fabric design.

2.4.5	Latex Additive: formulated for use in Portland cement mortars and grouts.

2.4.6	Organic Adhesive: to ANSI A136.1, Type [1] [2].

2.4.7	Water: potable, clean and free of chemicals and contaminants detrimental to mortar or grout mixes.

2.4.8	Thresholds: [______] marble, [______] mm thick, [rounded edges] [bevelled] [one side] [two sides], 			honed finish on exposed surfaces, size to suit door opening and frame width.

2.4.9	Transition Strips: purpose made metal extrusion; [stainless steel] [brass] [zinc] [anodized aluminum] 			type.

2.4.10	Reducer Strips: purpose made metal extrusion; [stainless steel] [brass] [zinc] [anodized aluminum] 			type; maximum of 1:2.

2.4.11	Prefabricated Movement Joints: purpose made, having a Shore A Hardness not less than 60 and 			elasticity of plus or minus 40 percent when used in accordance to TTMAC Detail 301MJ-2002.

2.4.12	Joint Sealant: as specified under Section 07900.

2.4.13	Seler: to CAN/CGSB-25.20, Type [1] [2]; as recommended by tile manufacturer.

2.5	MIXES

2.5.1	Scratch Coat (by volume): 1 part Portland cement, 4 parts sand, and latex additive where required 			by TTMAC Detail. Premixed mortar may be used per manufacturer’s instructions. Adjust water 				volume depending on moisture content of sand to obtain consistency and workability.

2.5.2	Slurry Bond Coat: mix Portland cement and water to a creamy paste consistency. Include latex 				additive where required by TTMAC Detail.

2.5.3	Mortar Bed for Walls (by volume): 1 part Portland cement, 4 parts sand and latex additive where 			required by TTMAC Detail. Premixed mortar may be used per manufacturer’s instructions. Adjust 			water volume 	depending on moisture content of sand to obtain consistency and workability.

2.5.4	Levelling Coat (by volume): Mortar Bed for Walls (by volume): 1 part Portland cement, 4 parts sand 			and latex additive where required by TTMAC Detail. Premixed mortar may be used per 					manufacturer’s instructions.

2.5.5	Mortar Bed for Floors: 1 part Portland cement, 4 parts sand, and latex additive where required by 			TTMAC Detail. Premixed mortar may be used per manufacturer’s instructions. Adjust water volume 			depending on moisture content of sand to obtain consistency and workability.

When mixed with water the mortar bad shall be of such a consistency and workability that will allow 			maximum compaction during tamping of the mortar bed, and achieve a minimum compressive 				strength of 15 MPa (2000 psi) after 28 days. A stronger mix can be achieve by adding latex to the 			water.

3.	Execution

3.1	EXAMINATION

3.1.1	Verify existing conditions are ready to receive work.

3.1.2	Ensure substrate surfaces are clean, dimensionally stable, cured and free of contaminants such as 			oil, sealers and curing compounds.

3.1.3	Ensure that concrete has been allowed to cure for a minimum of 28 days (preferably 90 days or 				longer].

3.1.4	Ensure concrete floor have not been treated with curing compounds.

3.1.5	Ensure concrete floors schedules to receive thin-set applied tile or cleavage membrane are steel 			trowelled to a fine broom finish. Ensure concrete slabs have been finished with a maximum 				permissible variation of 6 mm in 3049 mm from the required plane and not more than 2 mm in 305 			mm when measured from high points in the surface.

3.1.6	Ensure concrete floors scheduled to receive tile applied over a bonded mortar bed have been screed 			finished. Verify substrate surface variation does not exceed 6 mm in 3049 mm.

3.1.7	Notify Consultant in writing of unacceptable substrate conditions. Beginning of installation implies 			acceptance of existing conditions.

3.2	PREPARATION

3.2.1	Protect surrounding work from damage or disfiguration.

3.2.2	Thoroughly clean existing surfaces that are to receive tile finish to ensure the removal of all grease, 			oil or dust film.

SPEC NOTE: delete the following paragraph if no wood subfloor.

3.2.3	Securely screw underlayment to subfloor, smooth face up. Space sheets 6 mm apart.

3.2.4	Apply a latex cementitious levelling coat wherever a slight substrate irregularity exists. Limit levelling 			coat thickness to less than 8 mm where thin-set tile methods are to be used. A levelling coat in 				excess of 8 mm shall be set with a mortar bed method.

3.2.5	Install cleavage membrane over structural concrete slab. If a cleavage membrane is being applied 			over a rough surface, apply a 6 mm thick sand-bed under the cleavage membrane.

SPEC NOTE: Where finished tile floors are to be flush with adjacent floors, ensure that concrete slabs have been designed to be depressed the thickness of the mortar bed, bond coat and tile.

3.3	APPLICATION

3.3.1	Installation materials to requirements of TTMAC Tile Specification Guide, as scheduled below.

3.3.2	Fit tile units around corners, filments, fixtures, drains and other built-in objects to maintain uniform 			joint appearance.

3.3.3	Make cut edges smooth, even and free from chipping. Do not split tile.

3.3.4	Lay out tiles according to drawings and patterns so that perimeter and all cut tiles are no less that 			half size.

3.3.5	Prior to installation ensure that the back of each tile is free of contaminants.

3.3.6	For tile with raised or textured backs, bonding material must be evenly dispersed and pressed into 			the back of the tile to ensure a minimum of 95% coverage. Set tile in place while bond coat is wet 			and tacky, prior to skinning over. Notch bond coat in horizontal straight lines and set o the freshly set 			bonding material. Avoid lippage.

3.3.7	Clean excess bonding material from surface prior to final set.

3.3.8	Sound tiles after setting materials have cured and replace hollow sounding tile before grouting.

3.3.9	Use sufficient bond coat to ensure minimum 80% contact. Bonding material must be evenly 				dispersed and pressed into the back of the tile.

3.3.10	Bond coverage of 95% evenly dispersed is required for tile larger than 305 mm x 305 mm, tile used 			in wet areas or exterior, and for tile used in areas rated Heavy or Extra Heavy Duty. To help 				coverage [backbuttering] or [notch the bond coat in straight lines and move the tile back and forth 			perpendicular to notches when setting] are two techniques that can be used.

3.3.11	Keep two-thirds of depth of grout joints free of material.

3.3.12	Protect exposed edges of floor tile with appropriately sized transition strips. Provide reducer strips 			where uneven transitions between 6 mm and 12.5 mm occur.

3.4	CONTROL JOINTS

SPEC NOTE: Verify that the location of expansion, control, cold or seismic joints are indicated on the drawings. Use the following table to determine placement of control and expansion joints on the drawings. If not included on drawings, consider including table as part of specification.

Environment			Minimum		Maximum		Joint Width

Interior				4878 mm		6098 mm		6 mm minimum

Interior/Sunlight			3659 mm		4878 mm		6 mm minimum

Exterior – Normal		2439 mm		3049 mm		10 mm minimum

Exterior – Excessive		2439 mm		3049 mm		13 mm minimum

3.4.1	Install control joints and expansion joints in title work in accordance with TTMAC Detail 301MJ-2002.

3.4.2	Keep all control and expansion joints free of setting materials.

3.5	GROUTING

SPEC NOTE: Epoxy grout must be installed in a dust free environment and protected for 24 hours.

3.5.1	Allow proper setting time prior to grouting.

3.5.2	Pre-seal tiles requiring protection from grout staining.

3.5.3	Force grout into joints to ensure dense finish.

3.5.4	Remove excess and polish with clean cloths.

SPEC NOTE: Inspection may be part of the Verispec Program provided by the TTMAC.

3.6	FIELD QUALITY CONTROL

3.6.1	Inspect completed work and replace broken, cracked, hollow sounding or damaged tile.

3.7	TOLERANCES

3.7.1	Set and level tile flush with adjacent tile (lippage 1 mm tolerance over 3 mm joint).

3.8	CLEANING

3.8.1	Apply tile or stone sealer in accordance with manufacturer’s instructions.

3.9	PROTECTION

3.9.1	Protect finished area from traffic until setting materials have sufficiently cured. Refer to TTMAC Tile 			Specification Guide 09300/2002.

3.9.2	Protect grouted areas from traffic areas until substantial completion of the work.

3.9.3	Provide protective covering in traffic areas until substantial completion of the work.

3.9.4	Protect wall tiles and bases from impact, vibration, heavy hammering on adjacent and opposite walls 			for at least 14 days after installation.

3.10	SCHEDULE

SPEC NOTE: Specify TTMAC detail suitable for project. If more than one method applies, list conditions applicable to each detail.

3.10.1	Wall Tile: TTMAC Detail [____].

3.10.2	Floor Tile: TTMAC Detail [____].

3.10.3	Ceiling Tile: TTMAC Detail [____].

END OF SECTION